Student Self-Assessment Questions for Unit 4

These questions are included in the online reading in Student Materials

### Question 1

This table shows how long it takes for different minerals to dissolve (the solution rates of minerals).  From Drever, 1997 (pg. 233).

| Mineral | Time it would take a hypothetical 1 mm sphere of this mineral to dissolve in water with pH=5 (years) |
| --- | --- |
| calcite | 0.1 |
| olivine (forsterite) | 2300 |
| plagioclase (albite) | 575,000 |
| mica (muscovite) | 2,600,000 |
| clay (kaolinite) | 6,000,000 |
| quartz | 34,000,000 |

### Based on the table, which mineral is most soluble (dissolves most easily)?

### quartz

### olivine

### calcite

Question 2  Which of the following are examples of mechanical weathering?

- Water fills a crack in the pavement. Overnight, the water freezes (and expands), so the pavement cracks even more.

- A road crew used dynamite to blast away a hillside.

- A teaspoon of salt dumped into a pot of boiling water dissolves.

- The bumper of a 1989 Honda rusts.

- Sediments (rocks) carried in a stream smash against each other, breaking off edges and corners.

Question 3   This table shows some economic minerals found in clastic sedimentary deposits and their common uses. Keep in mind that specific gravity is a way of measuring density.

| Mineral | Commodity | Specific gravity | Some uses |
| --- | --- | --- | --- |
| various | gravel |  | construction |
| quartz | sand, silica | 2.65 (quartz) | construction, glass, computer chips |
| rutile, ilmenite | titanium | 4.18–4.25 (rutile), 4.7 (ilmenite) | white pigment (paint), titanium metal (airplanes) |
| chromite | chromium | 4.6 | stainless steel |
| rare-earth oxides | rare-earth elements (REE) |  | computer and television displays, fiber optic cables, magnets, catalytic converters in cars |
| cassiterite | tin | 6.8–7.1 | coating for tin cans, bronze |
| cinnabar | mercury | 8.10 | fluorescent lights, thermometers, production of chlorine |
| diamond | diamond | 3.5 | gemstones, abrasives |
| native copper | copper | 8.9 | wiring, antifungal and antibacterial chemicals |
| native silver | Silver | 10.5 | mirrors, photography, electronics |
| native gold | gold | 15–19.3 | jewelry, electronics, currency |
| native platinum | platinum | 14–19 | jewelry, catalytic converters in cars, dental equipment |

Question 3a  Imagine you have identically sized pebbles of the minerals below. Which one will be heaviest?

- Quartz

- Silver

- Copper

- Diamond

Question #3b  Which erosion agent is most likely to pick up and carry (erode) the mineral pebble you selected?

- A very fast moving stream

- A gentle ocean wave

Wind

- Question 4

This table shows concentrations of ions in different waters (composition of average seawater and brine from Great Salt Lake, Utah (from Drever, 1997) and freshwater (rain and river water; from Hem, 1985)).  In the ocean and the Great Salt Lake, evaporation removes water, leaving other ions behind.  This concentrates the ions (as you can see by comparing the amounts of ions in seawater and the Great Salt Lake with the ions in rain water and the Mississippi River).  Note that brines, like that in the Great Salt Lake, are saltier than seawater; and while all brines are saltier than seawater, different brines will contain different amounts of certain ions.

| Ion | Average seawater (mg/kg) | Great Salt Lake (mg/kg) | Rain water from Menlo Park, CA (mg/kg) | Mississippi River (mg/kg) |
| --- | --- | --- | --- | --- |
| chloride | 19,350 | 140,000 | 0.8–17 | 24 |
| sodium | 10,760 | 85,600 | 0–9.4 | 20 |
| sulfate | 2,710 | 16,400 | 0.7–7.6 | 51 |
| magnesium | 1,290 | 7,200 | 0.7–1.2 | 10 |
| calcium | 411 | 241 | 0.8–1.2 | 38 |
| potassium | 399 | 4,070 | 0 | 2.9 |
| bicarbonate | 142 | 251 | 4–7 | 113 |
| silica | .5–10 | 48 | 0.3–1.2 | 7.9 |

Question 4a Which brine in the table has the highest salinity (contains the highest concentrations of dissolved ions)?

- Rain water

- River water

- Ocean water

- Water from Great Salt Lake

Question 4b  Evaporite minerals readily form in the Great Salt Lake, and in the ocean. Why do minerals crystallize in these places?

- Because concentrations of ions are high in these places.

- Because little rain falls in these places.

- Because these bodies of water are very large.

### Because temperatures are very hot in these places.

### References

Drever, James I. 1997. The Geochemistry of Natural waters: Surface and Groundwater Environments, 3rd Edition.  Prentice Hall.

Hem, John D. 1985. Study and Interpretation of the Chemical Characteristics of Natural Water, 3rd Edition.  USGS Water Supply Paper 2254.